## Slide 1
T
Diego Ontiveros,
Francesc Viñes, Carme Sousa
Departament de Ciència de Materials i Química Fisica &
Institut de Química Teòrica i Computacional (IQTCUB),
Universitat de Barcelona
Exploring the Photoactive Properties of MXenes for Water Splitting

## Slide 2
Photocatalysis
2 H2O
+ O2
→ 2 H2
Pollutant degradation
Air & Water purification
Solar Cells
Medical treatment
Synthesis
Photo
catalysis
Energy
Environment
Biochem
MXenes (Mn+1XnT2)
Green Fuel generation

## Slide 3
Optimal Photocatalysis
J. Mater. Chem. A, 2025, 13, 3302-3316
Optimal Photocatalysis
Bandgap & Band Alignment
Optical Absorption
Exciton formation and separation
Excited State Reactivity
Stability

## Slide 4
2 H2O → 2 H2 + O2
Group III-VI
M
C or N
X
O, S, Se, Te, OH
F, Cl, Br, I, NH, H
T
1 to 3
n
ABC, ABA
stacking
HM/H, HMX, HX
T position
>4000 MXene structures
Mn+1Xn
Tx
MXenes
Bandgap Screening

## Slide 5
n
X
Group
T
Chart: Eg (eV)
| Sc | Y | Ti | Zr | Hf | V | Nb | Ta | Cr | Mo | W
ABC HM | 0 | 0 | 0 | 0.416 | 0.522 | 0 | 0 | 0 | 0 | 0 | 0
ABC HMX | 3.233 | 3.417 | 0 | 0.994 | 0.904 | 0.795 | 0.727 | 0.794 | 0.509 | 0 | 0
ABC HX | 3.011 | 3.349 | 0.864 | 1.2 | 1.22 | 0.797 | 0.855 | 0.941 | 0 | 0.428 | 0.598
ABA H | 0 | 0 | 0 | 0.4 | 0.537 | 0.874 | 0 | 0 | 0 | 0 | 0.56
ABA HMX | 2.913 | 3.085 | 0.831 | 1.196 | 1.135 | 1.175 | 0 | 0 | 0 | 0 | 0
ABA HX | 3.369 | 3.399 | 1.376 | 1.28 | 1.51 | 0.204 | 0 | 0 | 0.546 | 0.532 | 0.552
M2CS2
Chart: 
| Sc | Y | Ti | Zr | Hf | V | Nb | Ta | Cr | Mo | W
ABC HM | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABC HMX | 0.753 | 1.163 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABC HX | 0 | 0.352 | 0.032 | 0.438 | 0.546 | 0.406 | 0.23 | 0 | 0 | 0 | 0
ABA H | 0 | 0 | 0 | 0.542 | 0.565 | 0 | 0 | 0 | 0 | 0 | 0
ABA HMX | 0 | 0 | 0 | 0.452 | 0.473 | 0 | 0 | 0 | 0 | 0 | 0
ABA HX | 0 | 0 | 1.833 | 0.481 | 0.689 | 0 | 0 | 0 | 0.734 | 0.752 | 0.794
M3C2S2
Chart: 
| Sc | Y | Ti | Zr | Hf | V | Nb | Ta | Cr | Mo | W
ABC HM | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABC HMX | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABC HX | 1.614 | 1.678 | 0 | 0 | 0 | 0 | 0.412 | 0.548 | 0 | 0 | 0
ABA H | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABA HMX | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABA HX | 1.253 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.274
M4C3S2
Chart: 
| Sc | Y | Ti | Zr | Hf | V | Nb | Ta | Cr | Mo | W
ABC HM | 2.479 | 2.435 | 0 | 0.378 | 0.552 | 0 | 0 | 0 | 0 | 1.392 | 1.184
ABC HMX | 2.539 | 2.475 | 0.6 | 0.556 | 0.564 | 0.624 | 0 | 0 | 0.63 | 0 | 0
ABC HX | 2.429 | 2.381 | 0.66 | 0.674 | 0.55 | 0 | 0 | 0.426 | 0.158 | 0 | 0
ABA H | 2.315 | 2.463 | 1.438 | 0.764 | 0.648 | 0 | 0.48 | 0.166 | 1.576 | 0 | 0
ABA HMX | 2.529 | 2.659 | 1.138 | 0.008 | 0 | 1.766 | 0.626 | 0.568 | 2.247 | 0 | 0
ABA HX | 2.677 | 2.753 | 0.782 | 0 | 0 | 0.63 | 0.588 | 0.592 | 1.682 | 0 | 0
M2CCl2
Chart: 
| Sc | Y | Ti | Zr | Hf | V | Nb | Ta | Cr | Mo | W
ABC HM | 0 | 0 | 0 | 0 | 0 | 1.449 | 0 | 0 | 0.44 | 0 | 0
ABC HMX | 0 | 0 | 0 | 0 | 0.474 | 1.371 | 0 | 0 | 0 | 0 | 0
ABC HX | 0 | 0 | 0.62 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABA H | 0.73 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.39 | 0 | 0
ABA HMX | 0.84 | 0.812 | 0.266 | 0 | 0 | 0.642 | 0 | 0 | 0.522 | 0 | 0
ABA HX | 0.736 | 0.622 | 0.514 | 0 | 0 | 0 | 0 | 0 | 0.096 | 0 | 0
M2NCl2
Chart: 
| Sc | Y | Ti | Zr | Hf | V | Nb | Ta | Cr | Mo | W
ABC HM | 2.629 | 2.401 | 0.452 | 0.46 | 0.558 | 0 | 0 | 0 | 0 | 0 | 0
ABC HMX | 2.431 | 2.305 | 0.522 | 0.452 | 0.36 | 0 | 0 | 0 | 0.681 | 0 | 0
ABC HX | 2.234 | 2.261 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABA H | 2.497 | 2.187 | 1.495 | 1.393 | 1.565 | 0.574 | 0.236 | 0 | 0 | 0 | 0
ABA HMX | 2.545 | 2.347 | 0 | 1.409 | 1.449 | 0.699 | 0.629 | 0.322 | 0 | 0 | 0
ABA HX | 2.423 | 2.323 | 0.361 | 0 | 0 | 0.697 | 0.644 | 0.644 | 0 | 0 | 0
M2CH2
Chart: 
| Sc | Y | Ti | Zr | Hf | V | Nb | Ta | Cr | Mo | W
ABC HM | 1.342 | 1.504 | 0 | 0 | 0 | 0 | 0 | 0 | 0.452 | 0 | 0
ABC HMX | 1.644 | 1.81 | 0 | 0.244 | 0 | 0.358 | 0 | 0 | 0.45 | 0 | 0
ABC HX | 2.008 | 2.11 | 0.562 | 0.446 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABA H | 0.438 | 0.7 | 0 | 0 | 0 | 0.53 | 0.58 | 0.438 | 0 | 0 | 0
ABA HMX | 0.77 | 1.128 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
ABA HX | 1.238 | 1.504 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
M2C(OH)2
ABC HM
ABA H
ABC HMX
ABA HMX
ABC HX
ABA HX
% of cases with bandgap
4356 terminated
structures
945
semiconductors
Bandgap Screening

## Slide 6
J. Mater. Chem. A, 2023, 11, 13754–13764
Energy Environ. Mater. 2024, 7, e12774
4356 terminated
structures
945
semiconductors
243
65
Correct Alignment
10 Promising cases: Sc2CT2, Y2CT2 (T = Cl, Br, S, and Se), Y2CI2 and Zr2CO2
2.48 eV
2.44 eV
3.23 eV
3.42 eV
2.31 eV
2.36 eV
1.94 eV
2.26 eV
2.75 eV
3.21 eV
H2
H+
H2O
O2
10
Most stable
Band Alignment

## Slide 7
Stability
Energetical
Imaginary Phonons → Possible deformation or unstable structure
Chart: Energy (eV)
| Sc2CS2 | Y2CS2 | Sc2CSe2 | Y2CSe2 | Sc2CCl2 | Y2CCl2 | Sc2CBr2 | Y2CBr2 | Y2CI2 | Zr2CO2
 | -5.5171 | -5.5171 | -5.1584 | -5.1684 | -5.4105 | -5.4167 | -5.0879 | -5.1286 | -4.7705 | -7.6838
 | -4.9665 | -4.8671 | -4.2078 | -4.1588 | -7.8399 | -7.7719 | -6.7367 | -6.8411 | -5.3217 | -10.9716
Chart: Energy (eV)
| Sc2CS2 | Y2CS2 | Sc2CSe2 | Y2CSe2 | Sc2CCl2 | Y2CCl2 | Sc2CBr2 | Y2CBr2 | Y2CI2 | Zr2CO2
 | -5.5171 | -5.5171 | -5.1584 | -5.1684 | -5.4105 | -5.4167 | -5.0879 | -5.1286 | -4.7705 | -7.6838
 | -4.9665 | -4.8671 | -4.2078 | -4.1588 | -7.8399 | -7.7719 | -6.7367 | -6.8411 | -5.3217 | -10.9716
Dynamical
Slight
deformation
Broken
symmetry

## Slide 8
Optical Properties: Absorption coefficient
Good absorption in the visible range
Frequency dependent dielectric function
Optical absorption

## Slide 9
Optical Properties: STH efficiency
Chart: 
| Sc2CS2 | Sc2CSe2 | Y2CS2 | Y2CSe2 | Sc2CCl2 | Sc2CBr2 | Y2CCl2 | Y2CBr2 | Y2CI2 | Zr2CO2
 | 2.6168 | 4.1133 | 7.2242 | 6.2437 | 24.554 | 24.2429 | 41.8396 | 43.8007 | 46.5742 | 8.3469
Chart: 
| Sc2CS2 | Sc2CSe2 | Y2CS2 | Y2CSe2 | Sc2CCl2 | Sc2CBr2 | Y2CCl2 | Y2CBr2 | Y2CI2 | Zr2CO2
 | 34.4148 | 35.6943 | 37.8582 | 37.2148 | 20.2711 | 28.0313 | 33.4164 | 35.0779 | 46.0341 | 30.2639
Chart: 
| Sc2CS2 | Sc2CSe2 | Y2CS2 | Y2CSe2 | Sc2CCl2 | Sc2CBr2 | Y2CCl2 | Y2CBr2 | Y2CI2 | Zr2CO2
 | 0.90055 | 1.4682 | 2.735 | 2.3236 | 4.9774 | 6.7956 | 13.9813 | 15.3644 | 21.44 | 2.5261
Converting solar light into H2 fuel (assuming 100% efficiency). solar flux.
Solar-to-Hydrogen Efficiency (Upper limit)
VBM
CBM
H2O/O2
H+/H2

## Slide 10
J. Phys. Chem. Lett. 2023, 14, 3712−3720
H+/H2
H2O/O2
H2
H+
H2O
O2
h+
h+
e-
e-
e-
e-
VB
CB
E
hν
e-
Exciton Formation and Separation
VBM
CBM
Charge density separation
Charge carrier mobility

## Slide 11
Exciton Formation and Separation
VBM
CBM
Charge density separation
Spatial Overlap integral
Qualitative
Quantitative
Charge density separated into layers.
VBM → C layer
CBM → M layer
Thin 2D materials → Difficult separation → Heterojunction

## Slide 12
Exciton Formation and Separation
Charge carrier mobility
Relative mobilities between and different directions

## Slide 13
MXenes
(zig-zag)
(armchair)
dynamical stability
indirect bandgap
2.26 eV
visible light absorption
charge density separation
VBM
CBM
charge carrier mobility
Photocatalytic Assessment

## Slide 14
Diego Ontiveros,
Francesc Viñes, Carme Sousa
Departament de Ciència de Materials i Química Física &
Institut de Química Teòrica i Computacional (IQTCUB),
Universitat de Barcelona
Computational Study of MXenes for Water Splitting Photocatalysis
PID2021-126076NB-I0
TED2021-129506B-C22
2021SGR00079
QHS-2023-2-0017
QHS-2023-3-0012
CEX2021-001202-M

## Slide 15
Diego Ontiveros,
Francesc Viñes, Carme Sousa
Departament de Ciència de Materials i Química Física &
Institut de Química Teòrica i Computacional (IQTCUB),
Universitat de Barcelona
Computational Study of MXenes for Water Splitting Photocatalysis
JMCA paper
diego.ontiveros@ub.edu
Slides (with How To)

## Slide 16
IBIRON = -1
NSW = 0
Hybrid (PBE0, HSE06 …)
LHFCALC = .TRUE.
ISMEAR = -5
LORBIT = 11
NEDOS = lots (>5000)
EMIN, EMAX = -10, +10
LVTOT = .TRUE.
LDIPOL = .TRUE.
IDIPOL = 3 #z
DOSCAR
LOCPOT
,
How To: Bandgap and Band Alignment
Plane averaged electrostatic potential
DOS

## Slide 17
IBIRON = 8
NSW = 1
POTIM = 0.01
EDDIFF = 1e-8
LREAL = .FALSE.
ADDGRID = .TRUE.
NWRITE = 3
PREC = Accurate
$ mv CONTCAR POSCAR_unit_cell
$ phonopy -d --dim=“4 4 1” -c POSCAR_unit_cell
$ mv SPOSCAR POSCAR
$ VASP-DFPT calculation
$ phonopy –-fc vasprun.xml
$ phonopy BANDS.conf -c POSCAR_unit_cell
$ phonopy-bandplot --legacy -l band.yaml -o bands.png
How To: Dynamical Stability
Use phonopy: https://phonopy.github.io/phonopy/
# BANDS.conf
BAND_POINTS = 500
FORCE_CONSTANTS = READ
DIM = 4 4 1
BAND_CONNECTION = .TRUE.
BAND_LABELS = G M K G
BAND = k-path
0 0 0 0.5 0 0 1/3 1/3 0 0 0 0
1
2
2
1
vasprun.xml
FORCE_CONSTANTS
band.yaml
Zr2CO2

## Slide 18
LWAVE = .TRUE.
Hybrid (PBE0, HSE06 …)
LHFCALC = .TRUE.
How To: Optical Spectra
GS Single Point
www.vasp.at/wiki/index.php/Dielectric_properties_of_Si_using_BSE
WAVECAR
WAVECAR
WAVEDER
WAVECAR
WAVEDER
W*.tmp
ISTART = 1
LWAVE = .TRUE.
Hybrid (PBE0, HSE06 …)
LHFCALC = .TRUE.
ALGO = EXACT
NBANDS = NELECT*10
LOPTICS = .TRUE.
LPEAD = .TRUE.
OMEGAMAX = 10
Watch out!
Memory
(KPOINTS, NBANDS, vacuum)
K-point convergence
ISTART = 1
LWAVE = .TRUE.
ALGO = GW0
ENCUTGW = ENCUT/2
NELMGW = 1
NBANDS = NELECT*10
NBANDSGW = NELECT*2
NOMEGA = >=100
ISTART = 1
LWAVE = .TRUE.
ALGO = BSE
ANTIRES = 0
PRECFOCK = Normal
ENCUTGW = ENCUT/2
NELMGW = 1
NBANDS = NELECT*10
NBANDSGW = NELECT*2
NOMEGA >= 100
OMEGAMAX = 10
NBANDSO >= 4
NBANDSV >= 4
GW-BSE Approach. 4 steps, all single points (IBRION = 1, NSW = 0)
Virtual Orbitals
GW single shot
BSE

## Slide 19
How To: Charge Carrier Mobility
Deformation potential theory

## Slide 20
How To: Charge Density
GS Single Point
IBRION = -1
NSW = 0
ISTART = 1
Hybrid (PBE0, HSE06 …)
LHFCALC = .TRUE.
LPARD = .TRUE.
LSEPB = .TRUE.
LSEPK = .TRUE.
IBAND = VB CB
IBRION = -1
NSW = 0
LWAVE = .TRUE.
Hybrid (PBE0, HSE06 …)
LHFCALC = .TRUE.
WAVECAR
Extract VB, CB band index
from OUTCAR
k-points paths
2
Line
reciprocal
0.00 0.00 0.00 VB
0.50 0.00 0.00 CB
PARCHG.nb.nk
Extract VBM, CBM
k-points
from bandstructure
CD extraction
VESTA (or others)
VBM
CBM
PARCHG.VB.kVBM
PARCHG.CB.kCBM
www.vasp.at/wiki/index.php/Band-decomposed_charge_densities